## Modern Materials

Modern Materials

•	A goal for modern chemistry and chemists is to design materials with specific properties.

•	This is achieved by:

•	modifying natural materials.

•	synthesizing entirely new materials.

•	We can better understand the physical and chemical properties of materials by considering the atomic- and molecular-level structural features of the molecules.

Lecture Outline

1.  Classes of Materials

•	“Materials” are substances or mixtures of substances that are linked by chemical bonds.

•	The bonds may be strong (e.g., covalent, ionic, metallic) or weak (e.g., London-dispersion forces, dipole-dipole interactions, hydrogen bonds).

Metals and Semiconductors

•	Recall that atomic orbitals combine to make molecular orbitals.

•	The number of molecular orbitals in a molecule equals the number of atomic orbitals used to make the molecular orbitals.

•	Molecules with large numbers of atoms have a very large number of molecular orbitals.

•	There is essentially no separation between energy levels.

•	Continuous bands of energy states are formed.

•	The band structure of a solid consists of a set of bands separated by energy gaps.

•	Materials may be classified according to their band structure.

•	Metals

•	Examples include gold, silver, and platinum.

•	The band structure has the highest energy electrons occupying a partially filled band.

•	There is very little energy cost for electrons to jump to a higher unoccupied part of the same band.

•	As a result, metals are good electrical conductors.

•	Semiconductors

•	Examples include silicon, graphite, and germanium.

•	The band structure has an energy gap that separates totally filled bands and empty bands.

•	The band gap is the energy gap between a filled valence band and an empty conduction band.

•	The result is that semiconductors are conductive, but less so than metals due to the presence of the band gap.

•	The bonding in semiconductors is covalent-network, ionic, or a combination of the two.

•	Electrical conductivity may be influenced by doping.

•	Doping is the addition of small amounts of impure atoms to the semiconductors.

•	Doping yields different kinds of semiconductors.

•	n-type:  The dopant atom has more valence electrons than the host atom.

•	This adds electrons to the conduction band.

•	An example is phosphorous doped into silicon.

•	p-type:  The dopant atom has fewer valence electrons than the host atom.

•	This leads to more holes in the valence band.

•	An example is boron doped into silicon.

Insulators and Ceramics

•	Insulators have a band structure similar to semiconductors, but they have a much larger band gap.

•	The energy needed to bridge the gap is high (similar to that required to break a chemical bond).

•	As a result, insulators are not electrically conductive.

•	Examples include diamond and most ceramics.

•	Ceramics are inorganic solids that are hard, brittle, less dense than metals, stable at high temperatures, and resistant to corrosion and wear.

Superconductors

•	Superconductors show no resistance to the flow of electricity.

•	Superconductivity involves the “frictionless” flow of electrons.

•	Superconducting behavior only starts when  the substance is cooled below the superconducting transition temperature, Tc.

•	High temperature superconductors were discovered in 1987 (YBa2Cu3O7, yttrium-barium-copper oxide, Tc = 95 K)

•	The highest Tc discovered to date is 138 K for Hg0.8Tl0.2Ba2Ca2Cu3O8.33.

•	One potential use of superconductors is to carry electrical current without resistance in generators, motors, faster computer chips, etc.

•	The development of new high-temperature superconducting materials is an active area of research.

•	Superconducting materials exhibit the Meissner effect, in which they exclude all magnetic fields from their volume.

•	The Meissner effect causes permanent magnets to levitate over superconductors.

•	The superconductor excludes all magnetic field lines so the magnet floats in space.

•	A potential application is levitated trains (“maglev”).

•	The first superconducting ceramic was discovered in 1986.

•	It was a ceramic oxide containing yttrium, barium, and copper.

•	One of the most widely studied ceramic superconductors is YBa2Cu3O7.

•	Most superconductors require very low temperatures in order to function.

•	High-temperature superconductivity (high-Tc) will make the use of superconductors more commercially viable.

•	New superconducting materials are continually being discovered.

•	MgB2 and C60 reacted with an alkali metal  have been shown to exhibit a superconducting transition  below about 39 K.

2.   Materials for Structure

Soft Materials:  Polymers and Plastics

•	Polymers are molecules of high molecular weight that are made by polymerization (joining together) of smaller molecules of low molecular mass.

•	The building block small molecules for polymers are called monomers.

•	Examples of polymers include plastics, DNA, proteins, and rubber.

•	Plastics are materials that can be formed into various shapes, usually with heat and pressure.

•	Thermoplastic materials can be reshaped.

•	Recycling of polypropylene takes advantage of this property!

•	Thermosetting plastic materials are shaped by an irreversible process.

•	They are not readily reshaped.

•	Elastomers are materials that exhibit elastic or rubbery behavior.

•	If a moderate amount of a deforming force is added, the elastomer will return to its original shape.

Making Polymers

•	Many synthetic polymers have a backbone of C–C bonds.

•	Carbon atoms have the ability to form unusually strong stable bonds with each other.

•	Example:  ethylene H2C = CH2

•	Ethylene can polymerize by opening the C–C  double bond to form C–C  single bonds with adjacent ethylene molecules.

•	The result is polyethylene.

•	This is an example of addition polymerization.

•	Ethylene molecules are added to each other.

•	In condensation polymerization two molecules are joined to form a larger molecule by the elimination of a small molecule (like water).

•	An example of such a condensation reaction is when:

•	an amine (R–NH2) condenses with a carboxylic acid (R–COOH) to form water and an amide.

•	A biological example of this reaction is the linking of amino acids to form polymer chains–proteins!

•	A protein is an example of a copolymer–-a polymer formed from different monomers.

•	Another example of condensation polymerization is the formation of nylon 6,6.

•	Diamine and adipic acid are joined to form nylon 6,6.

Structural and Physical Properties of Polymers

•	Synthetic and natural polymers commonly consist of a collection of macromolecules of different molecular weights.

•	Polymers are fairly amorphous (noncrystalline).

•	Polymer chains tend to be flexible and easily entangled or folded.

•	They soften over a wide range of temperatures.

•	They may show some ordering.

•	The degree of crystallinity reflects the extent of the order.

•	Stretching or extruding a polymer can increase crystallinity.

•	The degree of crystallinity is also strongly influenced by average molecular mass:

•	Low-density polyethylene (LDPE), which is used in plastic wrap, has an average molecular mass of 104 amu.

•	High-density polyethylene (HDPE), which is used in milk cartons, has an average molecular mass of 106 amu.

•	We can modify the polymeric properties by the addition of substances with lower molecular mass.

•	Plasticizers are molecules that interfere with interactions between polymer chains.

•	These make polymers more pliable.

•	Bonds formed between polymer chains make the polymer stiffer.

•	Forming such bonds is referred to as cross-linking.

•	The greater the number of cross-links, the more rigid the polymer becomes.

•	Example: Natural rubber is too soft and too chemically reactive to be useful.

•	Vulcanization of rubber involves the formation of cross-links in the polymer chain.

•	Rubber is cross-linked in a process employing short chains of sulfur atoms.

•	Vulcanized rubber has more useful properties.

•	It is more elastic and less susceptible to chemical reaction than natural rubber.

Hard Materials:  Metals and Ceramics

•	The properties of metals make them particularly useful in everyday applications:  They are ductile, malleable, and highly conductive.

•	Ceramics are used in many applications.

•	They are used to make cutting tools, abrasives (e.g., SiC), supports for semiconductor integrated circuits, piezoelectric materials, and tiles for the space shuttle.

•	Ceramics are brittle.

•	Small defects developed during processing make ceramics weaker.

•	Sintering involves heating of very pure uniform particles (< 10–6 m in diameter) at high temperatures under pressure to force individual particles to bond together.

•	Tougher ceramics may be made by adding fibers to a ceramic material.

•	An example is SiC fibers added to aluminosilicate glass.

Making Ceramics

•	Sol-gel process is the  formation of pure uniform particles.

•	A metal alkoxide is formed [e.g., Ti(OCH2CH3)4].

•	Alkoxides contain organic groups bonded to a metal atom through oxygen atoms.

•	Formed by the reaction of a metal and an alcohol.

•	For example:

Ti (s) + 4 CH3CH2OH (l) ( Ti(OCH2CH3)4 (s) + 2 H 2(g)

•	A sol is formed by reacting the alkoxide with water [to form Ti(OH)4].

•	A sol is a suspension of extremely small particles.

•	A gel is formed by condensing the sol and eliminating water.

•	A gel is a suspension of extremely small particles that has the consistency of 	gelatin.

•	The gel is heated to remove water and is converted into a finely divided oxide powder.

•	The oxide powder has particles with sizes between 0.003 and 0.1 µm in diameter.

•	A ceramic object is formed from the powder.

•	It is compacted under pressure and scintered at high temperature.

3.  Materials for Medicine

•	A biomaterial is any material that has a biomedical application.

•	An example is a therapeutic or diagnostic use.

Characteristics of Biomaterials

•	Choice of biomaterial for an application is influenced by the chemical characteristics.

•	Biocompatibility:

•	A substance is biocompatible if it is readily accepted by the body without causing an inflammatory response.

•	The chemical nature and physical texture of the object are important.

•	Physical requirements:

•	The material must be able to withstand the physical stresses of use.

•	For example, materials used for hip-joint replacements must be wear-resistant.

•	Chemical requirements:

•	Must be medical grade.

•	Must be innocuous over the lifetime of the application.

•	For example, polymers can not contain plasticizers or other substances that might be released and cause a problem for the patient.

Polymeric Biomaterials

•	Our bodies are composed of many biopolymers.

•	Examples include proteins, polysaccharides (sugar polymers), and nucleic acids (DNA, RNA).

•	These have complex structures with many polar groups along the polymer chain.

•	The repeat unit often varies along the chain.

•	For example, in proteins the monomers are amino acids.

•	There are twenty different amino acids commonly found incorporated into proteins.

•	Man-made polymers are usually simpler.

•	One or two different repeat units may be used.

•	Often this contributes to the body's ability to detect these as “foreign objects.”

Examples of Biomaterial Applications

•	Heart Replacement and Repairs:

•	Aortic valve replacements have become common.

•	There are also mechanical valves.

•	They must be designed to avoid hemolysis (breakdown of red blood cells) and other complications that may result from roughness in the surface of the material.

•	They must be designed to become incorporated into the body's tissues (fixed in place).

•	Vascular grafts:

•	These are replacements of portions of diseased arteries.

•	Current materials still present the risk of blood clots.

•	Artificial tissue:

•	This is lab-grown skin used for tissue grafts in burn patients.

•	Artificial tissue is grown on a polymeric support or scaffold.

•	“Smart” Sutures:

•	These are biodegradable sutures that hydrolyze slowly.

•	Smart sutures can reversibly change their behavior in response to an external stimulus.

•	They are made of a thermoplastic polymer that shrinks when heated to body temperature or above.

•	Sutures may be loosely tied by the surgeon and then become appropriately taut when warmed to body temperature.

4.  Materials for Electronics

The Silicon Chip

•	Many modern devices rely on silicon wafers or “chips” containing complex patterns of semiconductors, insulators, and metal wires.

•	Silicon is inexpensive, abundant, fairly nontoxic, can be chemically protected with SiO2, and can be used to produce enormous nearly atomically perfect crystals.

•	The transistor is the basic unit of the integrated circuit.

•	Electrons move from semiconductor “source” to semiconductor “drain” when voltage is applied to a metal/insulator “gate.”

Plastic Electronics

•	Some polymers with delocalized electrons can act as semiconductors.

•	The 2000 Nobel  prize in chemistry was awarded to the discoverers of “organic semiconductors.”

Solar Energy Conversion

•	Semiconductors are also used in the production of solar energy cells.

•	If you shine light with an appropriate wavelength on a semiconductor, electrons are promoted to the conduction band, making the material more conductive.

•	This property is known as photoconductivity.

•	Solar panels are made from silicon.

•	A solar cell is formed by the junction of n-type and p-type silicon.

•	Sunlight promotes electrons from the n-type side to the p-type side.

•	This results in a current that can be used to power electrical devices.

5.  Materials for Optics

Liquid Crystals

•	Solids are characterized by their order.

•	Liquids are characterized by almost random ordering of molecules.

•	There is an intermediate phase where liquids show a limited amount of ordering.

•	Liquid crystals are substances that exhibit one or more ordered phases at a temperature above the melting point.

•	Example: The first systematic report of a liquid crystal was cholesteryl benzoate.

•	It melts at 145°C.

•	Between 145°C and 179°C cholesteryl benzoate is milky and liquid crystalline.

•	At 179°C the milky liquid suddenly clears.

•	Cholesteryl benzoate passes through an intermediate liquid crystalline phase.

•	It has some properties of liquids and some of solids.

•	The liquid flows (liquid properties) but has some order (crystal properties).

Types of Liquid-Crystalline Phases

•	Liquid crystal molecules are usually long and rodlike.

•	In normal liquid phases they are randomly oriented.

•	The three types of liquid crystalline phase depend on the ordering of the molecules.

•	Nematic liquid-crystalline phase (least ordered)

•	Ordered along the long axis of the molecule only.

•	Smectic liquid-crystalline phase

•	Ordered along the long axis of the molecule and in one other dimension.

•	Molecules that exist as nematic or smectic crystals are often fairly long relative to their thickness.

•	Smectic liquid crystals often contain C=N bonds and benzene rings that add stiffness.

•	Many contain polar groups.

•	Dipole-dipole interactions promote alignment of the molecules.

•	Cholesteric liquid-crystalline phase (most ordered)

•	Molecules are aligned along their long axis.

•	In addition, the molecules are arranged in layers.

•	Molecules in each plane are twisted slightly relative to molecules in neighboring layers.

•	Many of the molecules are derivatives of cholesterol.

•	An example is cholesteryl octanoate.

•	The molecules are long, flat, and rod-like with a flexible tail.

•	The flexible tail causes the twist between the layers.

•	The flexible tail usually contains many C–C bonds (e.g., the hydrocarbon tail in cholesteryl octanoate).

•	The rings in the cholesterol portion are not planar, but give the molecule a flat, sausage-like shape.

•	Changes in temperature and pressure cause ordering between layers to change.

•	This results in color changes.

Semiconductor Light-Emitting Diodes

•	LEDs are light-emitting diodes.

•	LEDs are used in many types of displays.

•	The mechanism of action is the opposite of that involved in solar cells.

•	A small voltage is applied to a semiconductor device with a junction between an n-type and a p-type semiconductor.

•	The junction forms a n-p diode, in which electrons flow only in one direction.

•	When a voltage is applied, electrons in the conduction band from the n-side combine at the junction with the holes from the p-side.

•	Light is emitted whose photons have energy equal to the band gap.

•	LEDs of different visible colors may be made by appropriately “tuning” the band gap.

•	Red, green, and blue LEDs are available.

•	Organic LEDs (OLEDs) have advantages over traditional LEDs.  They are lighter, more flexible, and may be brighter and more energy efficient.

6.  Materials for Nanotechnology

•	Nanomaterials have dimensions on the 1 – 100 nm scale.

Semiconductors on the Nanoscale

•	Semiconductor particles with diameters in the 1 to 10 nm range are called quantum dots.

•	Semiconductor band gaps change substantially with size in the 1 – 10 nm range.

•	The smaller the particle is, the larger the band gap.  Consider cadmium phosphide.

•	On a macrolevel it looks black.  The band gap is small and it absorbs most of the visible light.

•	When the particle is made smaller, the color changes until it looks white.

•	No visible light is absorbed.

•	The band gap is so large that only uv light can excite electrons to the conduction band.

•	By appropriately tuning the band gap of the quantum dots, all colors of the rainbow can be obtained from one material.

•	Quantum wires have also been produced.  A quantum wire is a semiconductor wire that may have a very long length but a diameter that is only a few nanometers.

Metals on the Nanoscale

•	The mean free path of an electron is the average distance it moves before bumping into something and is scattered.

•	The mean free path of an electron in a metal at room temperature is on the 1 – 100 nm scale.

•	Metals with particle sizes of 1 – 100 nm have unusual properties.

•	Unusual properties of metal nanoproperties that are being explored include applications in biomedical imaging and chemical detection.

Carbon Nanotubes

•	Carbon nanotubes are sheets of graphite rolled up and capped at one or both ends by half of a C60  molecule.

•	May be either multiwall or single-walled.

•	Multiwall tubes consist of tubes within tubes.

•	Single-walled tubes may be 1000 nm or longer but only 1 nm in diameter.

•	Carbon nanotubes may be made either semiconducting or metallic without the need for doping.

•	Applications being explored include the development of carbon-based electronic devices.